## Slide 1: Electro-chemo-mechanical model
Boundary Conditions
  Top surface
    Current density
    Pressure –
    Bottom Surface
    Fixed
    Voltage = 0 V (Li Metal)
  Left and right surfaces
    Periodic boundary conditions
Interface conditions
  Between Film and Li Metal
    Tied
    Free with frictional sliding
Electrolyte – LLZO – 10-4 S/cm
Film1 - 10-5 S/cm = Rct = 10 ohm-cm^2
Film2 - 10-7 S/cm = Rct = 100 ohm-cm^2

## Slide 2
Results --- Low Rct center, high Rct sides
M.J. Wang, R. Choudhury, J. Sakamoto, Characterizing the Li-Solid-Electrolyte Interface Dynamics as a Function of Stack Pressure and Current Density, Joule. 3 (2019) 2165–2178. https://doi.org/10.1016/j.joule.2019.06.017.
Stripping only

## Slide 3
Plating at 1.2mA/cm^2
More removal from in the middle (low Rct)
Pressure and Flux slowly go to 0 showing separation
Due to decreased contact area (overpotential) increases.
Plating 1.2 mA/cm^2

## Slide 4
Current = 0.4 mA/cm^2, Time = 215
Current = 0.4 mA/cm^2, Time = 340
Current = 0.4 mA/cm^2, Time = 240
Latest results Stripping
Simulation are underway as a function of temperature
Stripping Results